水滑石基臭氧分解催化剂性能研究

马嘉川1,2 ，郭明星1,\*，王胜2,\*，王树东2

1. 大连海事大学 环境科学与工程学院，辽宁 大连116026；

2. 中国科学院大连化学物理研究所 洁净能源国家实验室，辽宁 大连116023

Study on the performance of hydrotalcite-based ozone decomposition catalyst

MA Jia-chuan1,2，GUO Ming-xing1,\* ，WANG Sheng2,\*，WANG Shu-dong2

( 1．*College of Environmental Science and Engineering*, *Dalian Maritime University*, *Dalian* 116026, *China*；

2． *Dalian National Laboratory for Clean Energy*, *Dalian Institute of Chemical Physics*,

*Chinese Academy of Sciences*, *Dalian* 116023, *China*)

表S1不同LDH的金属元素组成

Table S1 Metal element composition of different LDH

|  |  |  |
| --- | --- | --- |
| Samples | Weight Content(%) by ICP-OES | Molar Ratio |
|  | A | B | A/B |
| Ni3Co | 37.81 | 12.75 | 2.98 |
| Ni3Mn | 39.58 | 12.24 | 3.03 |
| Ni3Fe | 38.60 | 11.31 | 3.25 |
| Co3Fe | 36.34 | 12.78 | 2.70 |



图S1 反应前后Ni3Mn-LDH和Co3Fe-LDH催化剂的XRD谱图

Fig S1 XRD patterns of Ni3Mn-LDH and Co3Fe-LDH catalysts before and after the reaction



图S2 反应后Ni3Co-LDH催化剂的XRD谱图

Fig S2 XRD pattern of Ni3Co-G catalyst



图S3 不同LDH催化剂的N2吸附-脱附等温线

Fig S3 N2 adsorption-desorption isotherms of different LDH catalysts



图S4 不同LDH的热重（TG）曲线

Fig S4 Thermogravimetric curves of different LDHs